## Slide 1
Misorientation ~ 25.7 °
Suppressed superconductivity across BCP’ed Nb grain boundaries
Z.H. Sung, P.J. Lee, A.A. Polyanskii, A. Gurevich, D.C. and Larbalestier
Applied Superconductivity Center, National High Magnetic Field Laboratory at Florida State University, Tallahassee, FL, 32310, USA
Bi-crystals from high purity, large-grain, Nb
Current transport through the single grain boundary (GB)
Observation of flux penetration along GB with magneto-optical (MO) imaging
Measurements of surface topology with CLSM (Confocal Laser Scanning Microscope), Microstructure analysis with transmission electron microscopy and direct transport across the same GB in the superconducting state
Description of samples
Large grain Nb sheet from JLAB
Fig. 1. Overview of the as-received niobium slice from CBMM Ingot
One full slice, 3.1mm thick, cut from CBMM ingot was provided to our group by TJNAF for experimental analysis.
In this combined top and bottom image, Red arrow indicates “thinner” GBs have planes which are closer to the surface perpendicular. Blue arrow indicates “thicker-appearing” GBs are inclined ~25-30° from the perpendicular.
This as-received slice (RRR ~280, 3.1mm thick) has a very large grain size (~50-100mm), which allowed us to isolate multiple bi-crystals.
Sample preparation
Isolated different single & bi-xtal samples with wire-EDM as indicated in Fig. 1.
  Red rectangle for MO imaging and atomic-scale structure analysis
  Blue rectangle for transport measurement
    I-shaping (Dog-bone) → mechanical polishing → typical cavity inner surface treatments
Surface treatment after EDM cutting
  BCP (Buffer Chemical Polishing) treatment
    HF (48%) : HNO3(69.5%) : H3PO4 (85%) = 1:1:2 ratio
    Aggressively etch away the grain boundary so that a big groove is created at the grain boundary
  EP (Electropolishing) treatment
    HF (48%) : H2SO4(96%) = 1:9 ratio
    Voltage = 10-15V & Current density = 30 to 100 mA/cm2
    Relatively uniformly remove surface layers
Non-uniform flux penetration into bi-xtal (100min BCP).
H = 60mT
T=6K H = 0mT
ZFC
Remnant state
H = 120mT
Top & Bottom
Height profile at GB
5mm (W) × 6.1mm (H) × 3.1mm (T)
T=6K
~23.6° tilted GB
MO imaging on tilted GB
Transport measurement
Transport current applied to chemically treated Single & Bi-crystal samples in a function of perpendicular magnetic field (at Temp 4.2K)
Surface image of I-shape sample after BCP treatment
Surface Conditions
1. BCP'ed Single & Bi crystals
2. EP'ed Bi crystals
3. Artificially grooved BCP'ed single crystal (by FIB - Carl Zeiss 1540 Esb)
4. Ultra finely flattened Bi crystal.
* All Bi-crystals were isolated from the same GB (Misorientation ~ 26°)
E-J characteristics of BCP'ed Nb
Single crystal
Bi crystal
Deep groove on the surface
E-J curve of BCP'ed Single crystal-like intra grain-indicates a typical smooth curvature of superconducting transition from negative to positive with increase H.
Yet, the curve of BCP'ed bi-crystal-like intra grain-shows pronounced grain boundary resistance due to flux flow along GBBCP from Hext≈0.08T
H = 58 mT
FC T=6K
H = 0 mT
ZFC T=6K
H = 72 mT
H = 0 mT
FC T=6.5K
BCP'ed
EP'ed
ZFC T=6.5K
Reduced thickness sample (GB//Hext)
Same GB & thickness sample (GB//Hext)
Microstructure Analysis
GB
TEM was used to observe the vicinity of the GB after BCP treatment
Using FIB (Carl Zeiss 1540 Esb), we prepared TEM lamellae from the GB of the same sample after MO imaging
Double cap layers (Au-Pd & C) protected the surface Nb-O layers from radiation damage of FIB source
GB
GB
Au-Pd
C
Au-Pd
Oxide
Oxide
No oxide indentation at the GB
Thickness of Nb oxide; ~ 5-7nm
ACKNOWLEDGMENTS
High-purity, large-grain niobium sheet was provided by TJNAF.
This work was supported by the US DOE under grants DE-FG02-06ER41450,
DE-FG02-07ER41451 FNAL PO 570362 and the state of Florida.
Nb GBs show evidence for preferentially flux penetration (external dc magnetic field parallel to the GB plane) using Magneto Optical imaging.
Measured E-J characteristics for BCP'ed and mechanically flattened Nb Bi-crystals show a clear evidence for grain boundary weakness due to preferential flux flow along the GB.
Our data indicate that pinning of vortices along GBs is weaker than pinning of vortices in the grains, which may indicate suppressed superfluid density on GBs, which thus can contribute to enhanced rf losses in hotspots on the surface of Nb cavities.
However, flux flow resistivity RF(H) extracted from our data deviates from the model developed by Alex Gurevich for the flow of AJ vortices along the grain boundary on HTS. This may be due to shape effects and further experiments are underway to make direct measurements of the local magnetic flux density.
 | 1st linear fitting |  |  | 2nd linear fitting | 
H [T] | W [μm] | dV | a [10-7] | W [μm] | dV
0.08 | 0.19 | 1.15 | 1.61 | 0.49 | 3.04
0.10 | 0.36 | 2.51 | 1.44 | 0.12 | 8.38
0.13 | 0.44 | 3.52 | 1.26 | 0.26 | 20.61
0.15 | 0.48 | 4.04 | 1.17 | 0.30 | 25.41
0.18 | 0.48 | 4.44 | 1.07 | 0.34 | 31.31
0.20 | 0.49 | 4.85 | 1.02 | 0.35 | 34.57
0.23 | 0.60 | 6.32 | 9.48 | 0.40 | 41.97
0.25 | 0.68 | 7.44 | 9.10 | 0.44 | 48.17
Summary
Flux flow resistivity RF(H)
Linear scale of BCP'ed Bi Xtal
Suppression of superconducting properties not as clear for EP’ed GB.
For an artificial groove, simulating BCP’ed GB topology on theBCP’ed Single crystal, we do not observe the same change in the VI-curve that is associated with flux-flow resistivity in the grain boundary.
E-J characteristics of EP'ed Bi-crystal & Artificially FIB grooved Single-crystal
EP'ed Bi-Xtal
Artificially grooved Single Xtal
Uniform surface
Deep groove
BCP’ed
SE2 image
Surface topology
Surface topology
Courtesy of A. Gurevich
ρn = the normal state resistivity A = the cross-sectional area W (H, J) = the width of vortices channel, which exceeds the inter-vortex spacing a=(Ф0/H)1/2 dVrow = the number of the vortex rows on the channel.
,
1
4
t
h
I
n
t
e
r
n
a
t
i
o
n
a
l
C
o
n
f
e
r
e
n
c
e
o
n
R
F
S
u
p
e
r
c
o
n
d
u
c
t
i
v
i
t
y
S
e
p
t
e
m
b
e
r
2
0
-
2
5
,
2
0
0
9